## Slide 1
Achieving Optimum Scientific Standards for Designing and Producing Fabrics Suitable for Ultraviolet Protective Clothing
Journal of American Science, 2011;7(9)
http://www.americanscience.org
Ibrahim, G., E.,
Abstract
This research is mainly concerned with producing woven cotton fabrics used in Ultraviolet Protective Clothing. The produced fabrics were treated with UV-Fast AO. Different parameters were studied including, Their influence on the performance of the end-use fabric and the achieved properties were studied. Some more results were reached concerning structures and materials. Most samples have achieved the expected results
U.V resistance
It can be also seen from tables and figures that treatment of fabrics led to improvement in properties of the U.V resistance. It was found that treatment of the fabrics provided good U.V resistance and it decreases with the increase of the exposure periods. So samples after three hours exposure have recorded the lowest rates of resistance rate against U.V. compared to samples of one hour exposure.
Fabric handle
It can be seen from the table and figures that the more yarn count number, the fabric become the samples become. I can report that the increase in this factor increase number of yarns leading the fabric to be more compacted which cause the increase the smoothness
Air permeability
It is clear from the diagrams that plain weave 1/1 has obtained the highest rates of air permeability, whereas satin 6 has obtained the lowest rates, and this is for sake of the increase of the pores in plain weave structure compared to satin structure which lead the produced fabric to be more permeable causing the increase in the air permeability.
Results
Hira, M., A., "Fire-resistant Clothing and its Performance Testing", The Indian Textile Journal, July, 2003.p39
2- Adanur, S., ‘Wellington Sears Handbook of Industrial Textiles’, 1st edition, Wellington Sears Company, Lancaster, Pennsylvania. 1995, p 415
4-Schindler, W., D., and Hauser, P., J.," Ultraviolet Protection Finishes", Chemical Finishing of Textiles, 1st edition ,Woodhead publishing Ltd.in association with The Textile Institute, Cambridge, England,2004. p 157-
5-Gorensek, M., and Sluga , F., " Modifying the UV Blocking Effect of Polyester Fabrics", Textile Research Journal , vo/l.74 , no. 6, 2004.p469
References
Experimental Work
This research concerns with producing fabrics suitable for ultraviolet protective clothing. All samples in the research were produced with cotton yarns using three woven structures ( plain weave 1/1,twill 3/3 and satin 6) .Three weft sets were also used (24,30 and 36 pick /cm) , using two different yarn counts (30/1 and 40/1 English )
Tests applied to samples under study
Several tests were carried out in order to evaluate the produced fabrics
Finishing treatment
Samples under study were coated with UV- Fast AO with 15 % concentration as follows:
The fabric samples were padded in an aqueous solution containing UV-Fast AO which is nonionic wetability substance (ejetol) and then squeezed to a wet pick up 100 %.after that samples were dried at 40 0 C for 20 min ,then thermo-fixed at 110 0 C for 20 seconds.
Methods and Materials
Introduction
Fabrics used in UV protection
Designing and modifying fabrics to offer high protection against ultraviolet (UV) radiation is a relatively new application, (6) and is considered one of the most important element in preventing skin cancer. Owing to their low weight, cotton fabrics especially viscose fabrics made from filament yarns, are ideal for summer clothing and enjoy a high degree of acceptance among consumers. (6)
The construction of woven and knitted fabrics and the fiber type have a great influence on protection from ultraviolet transmittance. (5) The ultraviolet protection factor (UPF) of a fabric depends also on spaces between fibers and yarns , fabric color , finishing processes , the presence of additives , and laundering.(6)
Mechanism of UV protection
When radiation strikes a fiber surface, it can be reflected, absorbed, transmitted through the fiber or passed between fibers. The relative amount of radiation reflected, absorbed, or transmitted depend on many factors, including the fiber type, the fiber surface smoothness, the fabric cover factor and the presence or absence of fiber debutants , dyes and UV absorbers.
Fabric specifications |  |  |  |  |  |  | 
Sample No. | Yarn type | Fabric structure | Yarn count ( English ) |  | Warp set | Weft set | Finishing
 |  |  | Warp | Weft |  |  | 
1 | Cotton | Plain weave 1/1 | 80/2 | 30/1 | 40 | 24 | Treatment with UV-Fast AO
2 | Cotton | Plain weave 1/1 | 80/2 | 30/1 | 40 | 30 | Treatment with UV-Fast AO
3 | Cotton | Plain weave 1/1 | 80/2 | 30/1 | 40 | 36 | Treatment with UV-Fast AO
4 | Cotton | Plain weave 1/1 | 80/2 | 40/1 | 40 | 24 | Treatment with UV-Fast AO
5 | Cotton | Plain weave 1/1 | 80/2 | 40/1 | 40 | 30 | Treatment with UV-Fast AO
6 | Cotton | Plain weave 1/1 | 80/2 | 40/1 | 40 | 36 | Treatment with UV-Fast AO
7 | Cotton | Twill 3/3 | 80/2 | 30/1 | 40 | 24 | Treatment with UV-Fast AO
8 | Cotton | Twill 3/3 | 80/2 | 30/1 | 40 | 30 | Treatment with UV-Fast AO
9 | Cotton | Twill 3/3 | 80/2 | 30/1 | 40 | 36 | Treatment with UV-Fast AO
10 | Cotton | Twill 3/3 | 80/2 | 40/1 | 40 | 24 | Treatment with UV-Fast AO
11 | Cotton | Twill 3/3 | 80/2 | 40/1 | 40 | 30 | Treatment with UV-Fast AO
12 | Cotton | Twill 3/3 | 80/2 | 40/1 | 40 | 36 | Treatment with UV-Fast AO
13 | Cotton | Satin 6 | 80/2 | 30/1 | 40 | 24 | Treatment with UV-Fast AO
14 | Cotton | Satin 6 | 80/2 | 30/1 | 40 | 30 | Treatment with UV-Fast AO
15 | Cotton | Satin 6 | 80/2 | 30/1 | 40 | 36 | Treatment with UV-Fast AO
16 | Cotton | Satin 6 | 80/2 | 40/1 | 40 | 24 | Treatment with UV-Fast AO
17 | Cotton | Satin 6 | 80/2 | 40/1 | 40 | 30 | Treatment with UV-Fast AO
18 | Cotton | Satin 6 | 80/2 | 40/1 | 40 | 36 | Treatment with UV-Fast AO
UPF of samples before exposure |  |  |  |  |  | The test
Satin 6 |  | Twill 3/3 |  | Plain weave 1/1 |  | Fabric structure
40 | 30 | 40 | 30 | 40 | 30 | Yarn count Weft set
1.6 | 1.7 | 1.7 | 1.9 | 2.1 | 2.8 | 24
1.8 | 2.5 | 2.0 | 2.1 | 2.6 | 4.6 | 30
2.2 | 2.8 | 2.5 | 3.2 | 4.3 | 4.9 | 36
Handle ( 0) |  |  |  |  |  | The test
Satin 6 |  | Twill 3/3 |  | Plain weave 1/1 |  | Fabric structure
After treatment | Before treatment | After treatment | Before treatment | After treatment | Before treatment | Weft set
41 | 37 | 40 | 38 | 42 | 39 | 24
43 | 39 | 41 | 39 | 43 | 40 | 30
44 | 40 | 43 | 41 | 45 | 41 | 36